| Project | Quality Indicators | Test Method |
| --- | --- | --- |
| Apprence | A viscous suspension, milky white to light yellow in color. | Visually |
| Calcium concent % NO less. | 17 | SH/T0309-1992 |
| Density：g/cm³ | 0.90-1.20 | GB-2013-2010 |